The Hardware Floor:  (no diamonds)

New, Hard-Trowelled floors

1. Clean surface with cleaner and water and some kind of agitation (use of stripper pads is ideal) to remove any loose material. 

2. Apply Lythic Densifier – keep wet for 15-minutes

3. After it dries, remove dried material by cleaning again – using stripper pads and water.

Allow to damp dry.

4. Apply Lythic XL Densifier – keep wet for 15-minutes

5. After it dries, remove dried material by cleaning again – using stripper pads and water

6.  Once completely dry burnish concrete. Or you can apply Lythic Protector and then burnish 	with high-speed burnishing pad. Hogs Hair or Green Twister pads are an option.

This system is for durable, non-dusting, harder wear surface that may not want or need a 	high polish.

Existing slabs

1. Grind to remove residues and hone at 80 - 100-grit resin.

2. Apply Lythic Densifier – keep wet for 15-minutes

3. After it dries, remove dried material by cleaning again – using stripper pads and water.

Allow to damp dry.

4. Apply Lythic XL Densifier – keep wet for 15-minutes

5. After it dries, remove dried material by cleaning again – using stripper pads and water

6.  Once completely dry burnish concrete. Or you can apply Lythic Protector and then burnish  	with high-speed burnishing pad. Hogs Hair or Green Twister pads are an option.

This system is for durable, non-dusting, harder wear surface that may not want or need a 	high polish.

Optional Protector Application

Apply Lythic Protector with a microfiber mop or pad applicator. You can dilute more than normal and apply twice to get even coverage.  An even coverage is important.

Burnishing

Once completely dry use floor stripper pads to smooth out the Protector barrier (Black Stripper Pad). Then burnish with Hogshair pad or similar.

OR
Use diamond impregnated pads will do the same as the 2-step process as described above. (Green Twister pads are one option)

Burnish with a minimum 2000 RPM machine.

Burnish to achieve a min concrete surface Temp of 32C. A hand held digital temperature device model number is QM7215 from Jaycar is ideal to ensure a min Temp of 32C is achieved. Available from Jaycar 16-18 Fisher Crescent Mt Wellington, Ph. 0800 452 922.

Allow finished floor to cure for 24 hours before allowing regular foot traffic. Wait 72 hours     before leaving standing water.

 Protector is only for Indoor usage.

Reapplying Protector and burnishing can renew the shine.

www.concretesealers.co.nz