Hardware Floor:  (no diamonds)

1. Clean surface with some kind of agitation to remove any loose material (use cleaner if required).

2. Apply Lythic Densifier – keep wet for 15-20 minutes

3. After it dries, remove dried material by cleaning again – using stripper pads and water

4. Apply Lythic XL Densifier – keep wet for 15-20 minutes

5. After it dries, remove dried material by cleaning again – using stripper pads and water

Exposed Aggregate Floor

Diamond polish #1:

1. Grind with metal bond diamonds to expose aggregate.

2. Float cementitious skim coat product over the floor to fill pin holes.

3. Using diamonds after your next grind approx 400 grit apply Lythic Densifier as per instructions

4. Let dry after the 20 minutes dwell time.  No need to clean up excess.

5. Then polish to your usual ending grit.

6. Apply one thin application of Protector (optional). After 1 or 2 hours burnish. Achieve Temp of 	32C. Again, the pad you use will have an impact on the shine.

Diamond polish #2

1. Grind with metal bond diamonds to expose aggregate.

2. Float cementitious skim coat product over the floor to fill pin holes.

3. Using diamonds after your next grind approx 400 grit apply Lythic Densifier as per instructions

4. Let dry after the 20 minutes dwell time. No need to clean up excess.

5. Then polish to your usual ending grit.

6. Apply one thin application of Lythic XL Densifier. Do not pour on floor, but rather	either spray apply 	and spread or use pad applicator. Micro-fiber applicator will help prevent streaking an even layer 	application is important.

After drying, try either one, or all three of the next steps:

- Go over area with final diamond again. Done

- Go over area with final diamond and burnisher. Done

- Go over area with just burnisher. Done

One thin application of Protector can be applied (optional). After 1 or 2 hours burnish. Achieve Temp of 32C The pad you use will have an impact on the shine.