The Hardware Floor: (no diamonds)  Once floor has cured typically 21-28 days

New, Hard-Trowelled floors

1. Clean surface with cleaner and water if possible and some kind of agitation (Use of stripper pads is ideal) to remove any loose material You can vacuum or sweep or Burnish. An auto scrubber works best using stripper pads and water where water can be used to eliminate any dust.

2. Apply Lythic Densifier – keep wet for 15-minutes

3. Prior to floor being fully dry, clean using stripper pads and water. Allow to damp dry. Tip- using Lythic Cleaner to clean in the process will improve the clarity of the concrete.

4. Apply Lythic XL Densifier (can be diluted 5:1 for this application)– keep wet for 15-minutes

5. Prior to floor being fully dry, clean again as step 3.

6. Once completely dry burnish concrete. Or you can apply Lythic Protector and then burnish with high-speed diamond impregnated burnishing pad. Hogs Hair or Green Twister pads are   an option.

This system is for durable, non-dusting, harder wear surface that may not want or need a high polish.

Existing slabs

1. Clean surface with cleaner and water if possible and some kind of agitation, (aggressive pad or sanding screen) or, Grind to remove residues with 80 - 100-grit resin if necessary.

2. Apply Lythic Densifier – keep wet for 15-minutes

3. Prior to floor being fully dry, clean using stripper pads and water. Allow to damp dry. Tip- using Lythic Cleaner to clean in the process will improve the clarity of the concrete.

4. Apply Lythic XL Densifier (can be diluted 5:1 for this application)– keep wet for 15-minutes

5. Prior to floor being fully dry clean again as step 3.

6. Once completely dry burnish concrete. Or you can apply Lythic Protector and then burnish with high-speed diamond impregnated burnishing pad. Hogs Hair or Green Twister pads are   an option.

For a durable, non-dusting, harder wear surface that may not want or need a high polish.

www.concretesealers.co.nz

Optional Protector

Apply Lythic Protector. An even coverage is important. Surface should be completely clean and dry before application of Lythic Protector.

Use a microfiber mop or pad applicator. You can dilute more than normal and apply twice to get even coverage.

Using a low pressure pump sprayer, apply Lythic Protector in a light mist. Using a damp micro fibre or flat cotton pad applicator, spread Lythic Protector in a thin film coat using a figure 8 motion to reduce streaking and to prevent puddling. 

After 1 to 2 hours, Burnish. Burnishing with a minimum 2000 RPM machine.

For this burnish achieve a concrete surface Temp of 32C. A hand held digital temperature device is ideal for this purpose and can be purchased from Jaycar 16-18 Fisher Crescent Mt Wellington, Ph. 0800 452 922. Value is $62.00 – model number is QM7215

Allow finished floor to cure for 24 hours before allowing regular foot traffic. Wait 72 hours     before leaving standing water.

 Protector is only for Indoor usage.

Reapplying Protector and burnishing can renew the shine.

Cure finished floor for 24 hours before allowing regular foot traffic. Do not allow standing water to remain on the surface for the first 72 hours.

www.concretesealers.co.nz