NEW FLOOR PROCESS

DAY1 TREATED SLAB 

The technology of Colloidal Silica bonds with itself, a property not seen in any other product. 
This allows a slab treated with DAY1 be burnished to produce a permanently Densified, Dust Proofed, Abrasive Resistant floor with a Shine ceateing a slab with great aesthetics and ease of cleaning at a Low Cost with NO Grinding using the Lythic New Floor process.

DAY1 provides an ideal substrate to receive polishing/burnishing using the 
Lythic New Floor or Hardwear Floor or Exposed Aggregate systems.

Hardwear Floor (no grinding)
A Breakthrough Technology that provides a Densified, Dust Proofed, Abrasive Resistant floor with a Shine. 
View Hardwear Floor Process www.lythic.net/process/hardwear

Exposed Aggregate (polished floor)

To polish a slab treated with DAY1 protocol is as follows:
After 21-28 days proceed with standard Lythic Polishing protocols.

New Floor (burnishing)
The following 2 simple methods of treating concrete floors with the New Floor process.


STANDARD CURING METHOD

Using standard curing methods Lythic can deliver high quality durable finishes very economically.

Hardwear Floor (no grinding)
A Breakthrough Technology that provides a Densified, Dust Proofed, Abrasive Resistant floor with a Shine.
After 21-28 days proceed with standard Lythic Hardwear Floor protocols. 
View video of Hardwear Floor Process www.lythic.net/process/hardwear

Exposed Aggregate (polished floor)

After 21-28 days proceed with standard Lythic Polishing protocols.

New Floor

Place slab with standard methods.

Option 1:
Apply Lythic XL Densifier directly after pour.
After 21 – 28 days clean and burnish.
You can proceed to test burnish at an earlier date, say after 5 days. Burnish with minimum 2000 RPM machine
Apply Lythic Protector as an option to increase shine and stain resistance.

Option 2:
After 21 – 28 days Clean slab with water
Apply Lythic XL Densifier
Burnish with minimum 2000 RPM machine
Apply Lythic Protector as an option to increase shine and stain resistance

www.concretesealers.co.nz