LYTHIC FLOOR DAY1 Process

The following simple examples of treating concrete floors with the LYTHIC FLOOR DAY1 process.

This is a High spec and a Low cost process for Densifing and hardening concrete floors with a shine.

Option 1:
After 21 days Clean slab with auto scrubber and Red/Black pad and burnish with diamond impregnated pads with minimum 2000 RPM machine.

Option 2:
After 21 days Clean slab with auto scrubber and Red/Black pad
Apply Lythic Protector (application of Protector directly on DAY1 slab should be done only when moisture content is low and controlled) and burnish with diamond impregnated pads with minimum 2000 RPM machine. 
Burnish to achieve a min concrete surface Temp of 32C.

Option 3:

After 21 days Clean slab with auto scrubber and Red/Black pad

Apply Lythic Densifier or XL Densifier and burnish with diamond impregnated pads with minimum

2000-RPM machine. Option: Application of Lythic Protector for increased shine if required.

Clean slab with auto scrubber red/black pad and water once, completely dry apply Lythic Protector

and burnish with diamond impregnated pads with minimum 2000 RPM machine.

Option 4:

Apply Lythic Densifier or XL Densifier directly after pour.

After 21 days clean and apply Lythic Densifier and Burnish with diamond impregnated pads with

minimum 2000 RPM machine. Option: Application of Protector for increased shine if required.

Clean slab with auto scrubber red/black pad and water, once completely dry apply Lythic Protector

and burnish with minimum 2000-RPM machine

or

LYTHIC Floor Hardwear Floor (no grinding)

Breakthrough Technology that provides a Densified, Dust Proofed, Abrasive Resistant floor with a

Shine.

View Hardwear Floor Process video www.lythic.net/process/hardwear

or

LYTHIC Floor Exposed Aggregate (polished floor)

Lythic produces a better polish with ability to achieve higher shine finish with lower grit abrasives
www.concretesealers.co.nz/exposed-aggregate-system/

Application video of DAY1 -https://youtu.be/fVU-jmz3DPc

www.concretesealers.co.nz